## Slide 1: Exact Ab Initio Scattering for Photocathode and SRF Development Tyler Wu1, Cristóbal Méndez2, J. K. Nangoi1,3, Tomás Arias1 1Department of Physics, Cornell University, Ithaca, New York 14853, USA 2School of Applied and Engineering Physics, Cornell University, Ithaca, New York 14853, USA 3Materials Department, University of California, Santa Barbara, California 93106, USA
Notes: Scattering theory is critical in all aspects of accelerator physics, which is why I’m very excited to go over our new work on ab initio theory for photocathodes and SRF cavities.

## Slide 2: Talk Outline
Theme 1 Photocathodes: Ab initio one-step theory via time-reversed LEED states
Motivation
Theory
Ag 111 results
Theme 2 SRF Cavities: Exact helium atom scattering (HAS) states
HAS Motivation
Lippmann-Schwinger theory
Elastic and inelastic HAS results

## Slide 3: Talk Outline
Theme 1 Photocathodes: Ab initio one-step theory via time-reversed LEED states
Motivation
Theory
Ag 111 results
Theme 2 SRF Cavities: Exact helium atom scattering (HAS) states
HAS Motivation
Lippmann-Schwinger theory
Elastic and inelastic HAS results

## Slide 4: Motivation: Bright Electron Sources
Electron beams enable technologies like electron microscopy and accelerators
Performance is set by the brightness of the emitted beam
  Quantum efficiency (QE): electrons out/photons in
  Mean transverse energy (MTE): ~transverse spread
Key challenge: achieving high emission without degrading beam width
Quick materials screening enabled by first-principles calculations
Low QE
High MTE
Laser
Photocathode
High QE
Low MTE
Laser
Photocathode
Notes: First-principles calculations enable quick screening for new materials search

## Slide 5: Theory ingredients
Ab initio calculation requires several key ingredients:
Plane wave DFT code
Wannier-based Green’s function scattering states
  Vacuum Wannier functions provide a localized first-principles basis for constructing scattering states at solid–vacuum interfaces (Wu and Arias, arXiv:2603.14105, 2026).
Inelastic electron scattering
vacuum
surface
Notes: Mention efficiency in plane wave code due to convenience of FFTs!
Wannier based scattering states enabled by VWFs. Want credit!

## Slide 6: Transition matrix elements
Electrons in the material feel an attenuated field controlled by the refractive index
  Fresnel equations
  Ab initio refractive index
Light-matter interaction
Typical term
Surface sensitive term
Ag(111)
Notes: Not discontinuous, but rapidly varying

## Slide 7: Ag(111) Inverse LEED states
Real-space representation
Imaginary self energy exponentially attenuates the inverse LEED states
Near-threshold inelastic mean free path (IMFP) is about 2.3 nm
Phonon self energy is 10x smaller than the e-e contribution
Notes: Get rid of a and c

## Slide 8: Ag(111) vectorial effect
Overall scale for absolute QE is very good
Peaks in correct locations
Ag(111)
Notes: Change legend from This work to ab initio
Stress absolute

## Slide 9: Ag(111) transverse momentum distributions
Single-peaked near-threshold TMD
Experiment inconsistent with Karkare model
Karkare model: double-peaked cut
This work: ab initio scattering states recover central peak
Full matrix elements redistribute weight to low
Ag(111)
Notes: Get rid of the zero points

## Slide 10: Talk Outline
Theme 1 Photocathodes: Ab initio one-step theory via time-reversed LEED states
Motivation
Theory
Ag 111 results
Theme 2 SRF Cavities: Exact helium atom scattering (HAS) states
HAS Motivation
Lippmann-Schwinger theory
Elastic and inelastic HAS results

## Slide 11: Talk Outline
Theme 1 Photocathodes: Ab initio one-step theory via time-reversed LEED states
Motivation
Theory
Ag 111 results
Theme 2 SRF Cavities: Exact helium atom scattering (HAS) states
HAS Motivation
Lippmann-Schwinger theory
Elastic and inelastic HAS results

## Slide 12: Motivation: Helium-atom scattering
SRF cavity performance limited by Nb surface quality
Surface oxides, adsorbates, defects, and reconstructions
HAS as a non-destructive probe of outermost surface structure and e-ph coupling
First-principles scattering theory for microscopic interpretation

## Slide 13: Current ab initio inelastic HAS theory
Inelastic HAS: one-phonon scattering from DFT He–electron vertex
Scattering state approximation
Figure adapted from M. M. Kelley, R. Sundararaman, and T. A. Arias, Phys. Rev. Lett. 132, 016203 (2024).
Notes: Only keep top panel

## Slide 14: Current ab initio elastic HAS theory
Debye–Waller attenuation from surface phonons and hard-wall scattering
Shared approximation: simplified He scattering states
Missing ingredient: exact elastic wave functions and diffraction channels
Adapted from C. Méndez, C. J. Thompson, M. F. Van Duinen, S. J. Sibener, and T. A. Arias, Phys. Rev. Lett. 135, 196201 (2025).
Notes: Old method uses electron density to define contour for hard wall scattering approximation
Delete plot

## Slide 15: Missing piece: exact scattering state
Incident He plane wave as source
DFT He–surface potential as scatterer
Truncated Green’s function for open-boundary propagation
Krylov solve for exact elastic scattering state
Notes: Artificial image effects from interactions with periodic copies

## Slide 16: New inelastic intensities
Lowered intensities from optical phonon branches
Excellent agreement with experiment
Notes: Reveal the figures one by one
Remove d

## Slide 17: Exact elastic He scattering
DFT-constructed He–Nb(100) potential: SCAN + vdW corrections
Realistic surface physics: Beeby well depth and anti-corrugation
Exact elastically scattered He wave functions
New elastic observables: Bragg peaks beyond specular reflection
Notes: DFT potential is also a new feature!
Specular means G=0
Old method incapable for Bragg peaks
Thompson is a former CBBer

## Slide 18: References
T. Wu and T. A. Arias, “Vacuum Wannier Functions for First-Principles Scattering and Photoemission,” arXiv:2603.14105 [cond-mat.mtrl-sci] (2026). DOI: 10.48550/arXiv.2603.14105.
M. M. Kelley, R. Sundararaman, and T. A. Arias, “Fully Ab Initio Approach to Inelastic Atom-Surface Scattering,” Physical Review Letters 132, 016203 (2024). DOI: 10.1103/PhysRevLett.132.016203.
C. Méndez, C. J. Thompson, M. F. Van Duinen, S. J. Sibener, and T. A. Arias, “Ab Initio Electron-Phonon-Coupling Theory of Elastic Helium-Atom Scattering,” Physical Review Letters 135, 196201 (2025). DOI: 10.1103/mcgg-8hk8.