## Slide 1: Single Crystal Photocathodes: A Route to Ultimate Beam Brightness and New Photoemission Physics
- Siddharth Karkare (Lawrence Berkeley Lab)
Notes: Good morning everyone. Thanks to Ivan for the Introduction. Today I will be talking about how we plan to use single crystal photocathodes to obtain the ultimate beam brightness limited only by disorder induced heating and will also shed some light on the possibility of encountering new photoemission physics while doing so

## Slide 2: Brightness, Emittance and Disordered Cathodes
0
electrons
Ez (sets maximum electron density)
electron beam
Laser
Photocathode
All photoinjectors use cathodes with disordered surfaces (eg. Alkali-antimonides, polycrystalline metals, NEA-GaAs)
Energy
Vacuum Level
Fermi Level
Surface roughness and work function variations eventually limit MTE
Feng et al. Appl. Phys. Lett. 107, 134101 (2015)
Karkare and Bazarov, Phys. Rev. Applied 4, 024015 (2015)
Feng et al. J. Appl. Phys. 121, 044904 (2017)
Notes: References add name

## Slide 3: Photoemission from Single Crystals and ARPES
ARPES – Angle Resolved Photoemission Spectroscopy
Used for decades to ‘measure’ the band structure of single crystal solids with ordered surfaces
Conservation of Transverse Momentum
Conservation of Energy
Can we use/design materials with band structures that result in low MTE and high QE?
*http://research.physics.berkeley.edu/lanzara/research/ti.html

## Slide 4: Ag(111) Surface-state – A test case
Easy to prepare – Simple ion bombardment and annealing to 4500C
  Gives excellent LEED pattern and clean Auger spectrum
Intense surface state peak in PES experiments – Could imply good QE
Intensity
Surface state peak
F. Reinert et al., PRB, 63, 115415 (2001)
T. Miller et al., Surf. Sci. 376, 32 (1997)
Narrow momentum spread in ARPES – implies low MTE
Narrow Momentum Spread

## Slide 5: Ag(111) – QE and MTE
Conservation of energy
Conservation of transverse momentum
Projected band structure in direction transverse to surface
Karkare et al. Phys. Rev. B 95, 075439 (2017)
Karkare et al. Phys. Rev. Lett. 118, 164802 (2017)
One step photoemission model
RMS Transverse
Momentum (eV/c)
Excess energy (eV)
25 meV

## Slide 6: Route to Ultimate Beam Brightness
High-throughput Materials Search
Photocathode with ultimate beam brightness
Materials growth
Expert: Richard Hennig
- See poster by Joshua T Paul
Expert: Kyle Shen
electrons
electron beam
Laser
Photocathode

## Slide 7: PbTe(111) – A Potential Cold Electron Source?
Conservation laws and band structure dictate that MTE should be < 5 meV
Li and Schroeder https://arxiv.org/pdf/1704.00194.pdf
How good is our surface?
Flat terraces are mostly 1x1 terminated
Can we obtain defect free p-doped surfaces?
STM image of PbTe(111) surface
- Hines group (Cornell) – See poster by Erik Skibinski, Will DeBenedetti
Can many body scattering effects with phonons explain this behavior?
Arias group is exploring this possibility
- See poster by Kevin Nangoi
Theory
Measurement

## Slide 8: Low Energy Effects – New Physics
Long electron wavelengths
- Emitted electrons can see atomic defects
or steps at 10s of nm
Sudden approximation breakdown
- Emitted electrons interact with changes inside the surface
- time required by an electron to move one DeBroglie wavelength
Adiabatic limit?
Sudden Approximation
ARPES uses electrons above 1 eV kinetic energy
Our electrons are in the 10 meV range!!!

## Slide 9: 3-D Low Energy Electron Diagnostics
Delay Line
Detector
Cryostat
Electrostatic shield
Sample
Sample
Incident laser pulse (fs-ps)
Electrons drift towards detector
MCP stack
X, Y Delay lines
(x,y,t) of electron hitting the MCP
Enables complete characterization of energy-momentum distribution of photoemitted electrons to provide insight into photoemission process
<1 meV energy resolution expected
Will allow cooling of sample to ~20K

## Slide 10: Route to Ultimate Beam Brightness
Photoemission Characterization
Surface Characterization
Ab-initio Photoemission theory
Physics of Low Energy Photoemission
High-throughput Materials Search and growth
Photocathode with ultimate beam brightness
Bazarov, Padmore,
Shen, Musumeci
Hines, Padmore, Muller
Arias
Hennig, Shen
Thanks to -
CBB Beam Generation team members
LBL – Jun Feng, Weishi Wan
UIUC – T. C. Chiang
NSF and DOE for $$$

## Slide 11: Ag(111) – Momentum distributions
Measurement
Theory

## Slide 12: Momentotron images – Cu(111)
4.77 eV
4.82 eV
4.88 eV
4.94 eV
4.98 eV
5 eV
5.04 eV
5.10 eV
5.17 eV
5.19 eV
5.25 eV
5.32 eV
5.39 eV
5.77 eV
6.17 eV

## Slide 13: x cross-sections (normalized to incident power), MTE

## Slide 14: Y-cross section vs voltage
5.14 eV
5.74 eV
4.98 eV

## Slide 15: Energy momentum distributions
4.76 eV
4.67 eV
4.57 eV
4.53 eV
5.04 eV
Preliminary first results

## Slide 16
ARPES of n-doped PbTe(111)
Yan et al. PRL 112, 2014, 18601
Our sample is p-doped!!!