## Slide 1: Superconducting RF
Continuous bright beams with low emittance
However, the cryogenics plant is costly to build and maintain
Notes: SRF cavities made of niobium operating at 1.8 to 2.0 K provide continuous beams with a low emittance
A major cost driver is the price of the cryogenics facility

## Slide 2: The case for Nb3Sn
Parameter | Niobium | Nb3Sn
Transition temperature | 9.2 K | 18 K
Superheating field | 219 mT | 425 mT
Energy gap Δ/kbTc | 1.8 | 2.2
λ at T = 0 K | 50 nm | 111 nm
ξ at T = 0 K | 22 nm | 4.2 nm
GL parameter κ | 2.3 | 26
Green: tin
Red: niobium
Higher critical temperature
→ Operation at 4.2 K
Higher superheating field
→ Double the limit of niobium
Notes: Nb3Sn is an alternative to niobium
An A15 intermetallic alloy with a Tc of 18 K
With a higher Hsh, the ultimate gradient should be twice that of Nb

## Slide 3: Operation at 4.2 K
~$1M
~$50k
4.2K
2K
Going to 4.2 K reduces cryogenic cost and complexity
Notes: (COP – coefficient of performance)
The higher Tc of Nb3Sn means that the cryomodule power consumption at 4.2 K is low enough to operate there
Moving to 4.2 K liquid operation greatly simplifies things
We could even use a cryocooler, which would be very low maintenance

## Slide 4: Fabricating an Nb3Sn cavity
A 1.3 GHz single-cell is placed into the furnace
Notes: Nb3Sn is brittle and cannot be shaped
We coat using the vapour diffusion method
We put a Nb structure into a UHV furnace

## Slide 5: Coating method
Tin source ( 1250 °C )
Secondary heater
Tin crucible
Primary heater
Coating chamber
( 1100 °C )
Cavity/sample
Vacuum space
( < 10-5 Torr )
Nucleation agent ( SnCl2 )
Notes: A specially adapted UHV furnace with two hot zones, one contained within the other.
The cavity sits in the main hotzone
At the base lie a nucleation agent for coating prep and the source
The source is in the second hotzone

## Slide 6: Post coating
A coated cavity doesn’t look very different
Notes: - A coated cavity looks more matte, but otherwise not very different

## Slide 7: Exemplary cavities
Bath temperature of 4.2 K
But the difference in performance is significant
Notes: These are some of our best performing cavities operating at 4.2 K
We have Qs approaching or exceeding 10^10 at useable gradients

## Slide 8: Comparison to niobium
30× more efficient than Nb at 4.2 K!
Notes: This is 30 times more efficient than Nb at 4.2 K at useable gradients
This is the first time an “alternative” cavity has beaten niobium at useable gradients

## Slide 9: Pushing performance further
Great performance! But theory predicts we can do even better
Pushing to the maximum achievable cavity efficiency
Understanding the limitations on accelerating gradient
How does the Centre for Bright Beams contribute to improving Nb3Sn?
Notes: This performance is already relevant to today’s machines
We want to push harder for the best efficiency
But we should be able to do better, particularly in terms of accelerating gradient
The centre for bright beams provides talent that has and can still make significant contributions to this research

## Slide 10: Maximising efficiency
Surface resistance = RBCS + RResidual
Low for Nb3Sn at 4.2 K
Must be minimised!
Even 3-5 nΩ can make a big impact
Notes: The surface resistance determines the efficiency
It has two components, one of which is fixed by the temperature and the material (BCS)
The other, the residual, must be minimised

## Slide 11: Loss mechanisms
0 nΩ
16 nΩ
Trapped flux
Thin film regions
BCS Resistance
Ambient fields
Thermal gradients
Notes: At 4.2 K, our non-BCS contribution comes from trapped flux and thin film regions (I will explain later)
Trapped flux are vortices trapped in the cavity during cooldown
They come from ambient fields and thermal gradients

## Slide 12: Generation of thermal currents
Nb
Nb3Sn
HOT
COLD
Generated B field
Induced thermocurrent
Thermal gradients → Thermal currents → Magnetic flux
Notes: The bimetallic interface of Nb3Sn allows the generation of thermal currents in the presence of thermal gradients
This generates magnetic flux, which is trapped

## Slide 13: Field dependent sensitivity
Nb3Sn is more sensitive to trapped flux at higher fields
Notes: For each mG of magnetic flux trapped, you get a certain number of nano-ohms. In Nb3Sn, this value actually increases with accelerating field!

## Slide 14: Weak collective pinning scenario
RF field increases
    Vortex amplitude increases
        Increased losses
Flux vortex oscillating
CBB Contribution by:
James P. Sethna and
Danilo B. Liarte
Notes: The CBB collaboration has actually been vital in understanding why this happens. Sethna and Liarte have developed a “weak collective flux pinning” model that is able to describe this behaviour. Understanding the physics behind this behaviour is critical in trying to change it.

## Slide 15: Improving cool-down
Data: 200 mK/m, 5 mG ambient
Extrapolated: 100 mK/m, 1 mG ambient
Bath temperature of 4.2 K
Optimising cool-down ensures great performance
Notes: The knowledge we have gained on this phenomenon has allowed us to tailor the cooldown of a cavity to achieve exceptional performance.

## Slide 16: Thin film regions
Too thin Sufficiently thick
Nb substrate
Nb3Sn
400 nm
CBB Contribution by: David A. Muller and Paul Cueva
Notes: Another source of loss are thin film regions, where the film is too thin to screen the bulk from the RF field. The contributions from the Muller group have been instrumental in imaging such features using electron microscopy.

## Slide 17: Suppressing thin film regions
Red: too thin Blue: sufficiently thick
Not pre-anodised
Pre-anodised substrate
Growing the substrate oxide prior to coating suppresses the formation of thin film regions
Notes: Through the use of pre-anodisation we have succeeded in removing these regions, as can be seen in scanning electron microscopy.

## Slide 18: Performance improvement
Data taken at 4.2 K
Gain of ≈3 nΩ
Notes: Indeed, we do see a difference when all other factors are held equal. A gain of 3 nO may seem small, but here is a big impact

## Slide 19: Accelerating gradient
The ultimate gradient of a cavity is determined by the superheating field, at which flux enters and quenches superconductivity
In Nb3Sn, this field is 400 mT, or 90 MV/m in an ILC cavity
We are currently limited to 14-17 MV/m
Notes: The other frontier on which the CBB can make a big impact is understanding what the current limitation in our accelerating field is

## Slide 20: Investigating quench dynamics
Nb3Sn cavities are limited by a quench at a defect
But what kind of defect, and why?
Notes: By monitoring the temperature of the surface of a cavity during quench, we see that the quench is isolated to a defect

## Slide 21: Temperature at quench origin
Data strongly suggests flux entry
Notes: When we look at this region, we see sudden jumps in temperature near the quench field! This is very suggestive of early flux entry

## Slide 22: Tc suppresion
A depletion of only 3% reduces Hsh by 75%
Flux entry could occur at tin-depleted surface defects
CBB Contribution by: James P. Sethna and Danilo B. Liarte
Notes: What could cause this? Tc suppression could. Sethna and Liarte are experts on flux entry into superconductors, and have looked into how suppression could reduce the superheating field

## Slide 23: Tin-depletion in grains
Cross-section of the Nb3Sn RF surface
Grain boundary
CBB Contribution by: David A. Muller and Paul Cueva
Notes: In fact, in samples we have already seen depleted grains at the surface, as we can see in these images provided by the Muller group

## Slide 24: Understanding layer growth
Nb3Sn
Nb
Sn
We compare growth simulations to features seen in coupons and correlate these with RF performance
Simulations use Joint Density Function Theory
CBB Contribution by:
Tomas Arias and
Nathan Sitaraman
Notes: We need to be able to alter the prevalence of all these features to see how they affect the quench field. The contributions of the Arias group, with their DFT simulation code, are proving useful in understanding how the layer grows. As we combine these simulations with our sample measurements, it is becoming increasingly clear that it is the very early stages of the coating that seal its fate.

## Slide 25: Outlook and conclusion
Cavity efficiency
  We routinely get quality factors of >1010 at 4.2 K and gradients of >14 MV/m
Accelerating gradient
  Cavities are limited by localised defects
  Surface features are being correlated to growth simulations to understand layer growth and guide the coating recipe
Nb3Sn cavities have achieved the performance specifications demanded by modern machines
Notes: To summarise – in cavity efficiency, we are doing very well, and can push it quite close to the limit. In accelerating gradient, we are isolating the defect that causes quench and trying to figure out what causes it to occur

## Slide 26: Acknowledgements
Prof. Matthias Liepe
Prof. Tomas Arias
Prof. David A. Muller
Prof. James P. Sethna
Danilo Liarte
Ryan Porter
Paul Cueva
Nathan Sitaraman
James Maniscalco
James Sears
Greg Kulina
John Kaufman
Holly Conklin
Terri Gruber
with special thanks to
The Cornell Nb3Sn program is primarily supported by the U.S. Department of Energy